## Slide 1
Nathan Carlson | Nick Baker | The University of Alabama
ncarlson@crimson.ua.edu, nbaker2@ua.edu
Solder Void Impact on Power Device Thermal Impedance using Transient Thermal Analysis
r
Motivation
Solder voids underneath the chip require expensive equipment to remove. This is especially true for mass production and research labs.
Thermal impedance and lifetime are two key metrics of a power device.
At present, there is a relative scarcity of direct experimental evidence between voids and these key metrics.
Void percentage = 100% * voided area / total area
Tau Intensity Technique
Problem: The thermal resistance of the solder layer is difficult to isolate due to the variable resistance of other layers.
Solution: The impedance can be measured a short time after applying a heating current. This time should be a point when the heat flux through the solder is high but has not fully reached the lower layers. The Tau Intensity plot can help to select this time (about 2-5 multiples of the solder layer’s time constant).
Solder layer
Thermal Impedance Results
Voids have the most significant impact on thermal impedance on short timescales. This indicates that from a thermal perspective, void removal would help to protect against thermal transient conditions such as a temporary short circuit, but that voids do not have a strong impact on the steady-state thermal resistance.
Lifetime Results
Voids accelerate the growth of solder cracks. Modules with low voids showed much longer lifetimes.
COMSOL simulated image from [1].
References
[1] Bjørn Jørgensen, Asger & Christensen, Nicklas & Dalal, Dipen & Sønderskov, Simon & Bęczkowski, Szymon & Uhrenfeldt, Christian & Munk-Nielsen, Stig. (2017). Reduction of parasitic capacitance in 10 kV SiC MOSFET power modules using 3D FEM. 10.23919/EPE17ECCEEurope.2017.8098962.
Diode test module