## Slide 1
Impact of Solder Voids on Power Module Thermal Resistance Using Transient System Analysis
Nathan Carlson
Dept. of Electrical and Computer Engineering
The University of Alabama
ncarlson@crimson.ua.edu
Dr. Nicholas Baker
Dept. of Electrical and Computer Engineering
The University of Alabama
nbaker2@crimson.ua.edu

## Slide 2
Why do we care about Thermal Resistance?
=
High thermal resistance = large temperature difference needed to conduct losses
Excess heat leads to semiconductor or package failure
Lowering Rth allows for…
Cheaper / smaller cooling equipment
OR
Higher power output
OR
Higher reliability and lifetime
Fig 1. General Layout of Power Module. [1]

## Slide 3
Void Percentage Calculation
Fig 3. Selection of voided areas using Fill Tool method.
Fig 4. Void selection with Threshold method.
Traditional threshold method susceptible to chip tilt errors
Fill Tool Method
Capture Xray image of solder
Import into Photoshop
Use the fill tool to select voided areas*
Calculate the number of red pixels vs total pixels
*Fill Tool Threshold settings: 35, 27, 20, 13, 5. Use high settings for large voids and voids with highly contrasted edges.

## Slide 4
The Experiment
Voids cause an increase in the thermal resistance of a power module.
Hypothesis
: Model parameters
: Void percentage
: Predicted thermal resistance
Should be predicted by the equation:
Should be able to be modeled as an LTI system:
Fig 5. Foster network (a) and Cauer network (b) can be used as representations of LTI thermal systems [2].

## Slide 5
Sample Creation
Fig 6. Test sample construction.
10 Samples
Diode Information:
SAC 305 solder paste
‘X’ shaped stencil with 100um thickness
Reflow in convection oven: Manncorp MC 301
Two reflow profiles used (see appendix)
PCB surface metallization: bare Cu
Model: VS-4FD198H06A6BC
Size: 5.03mm X 3.35mm
Rated current: 50A

## Slide 6
Rth Test Setup
+ -
Diode Junction Temperature Calculation
Example Cooling Curve
Tested currents: 5, 10, 15, 20, 22, 24A

## Slide 7
Postprocessing: Extraction of Heating Curve
Goal: Given a cooling curve, calculate the heating curve
Assumption 1
Assumption 2
Thermal system is linear and time-invariant (LTI)
System reaches steady-state within 200 seconds
Thermal System
Thermal System
Cooling
Heating

## Slide 8
Postprocessing: Tau Intensity Calculation
Fig 7. Example diagram of heat flow through a power device [3].
Single Element
Lumped Element
Continuous
Increasing Accuracy
Step response
Equivalent circuit
Step response
Equivalent circuit
Step response
Equivalent circuit
Using , solve for the continuous Tau Intensity function using the method shown in [4].

## Slide 9
Postprocessing: Tau Peak Identification
Fig 8. Plot of Tau Intensity vs time, with peaks identified.
Purpose of Tau Intensity
Peaks of the tau intensity plot correspond to high R and low C relative to the surrounding region
The first tau peak (1.12 ms) corresponds to the first material junction from the chip to the solder layer
Thus, measuring Zth at ~1.12 ms should give more accurate measurements than in steady-state

## Slide 10
Results: First Tau Peak Distribution
Where does the first peak occur most often?
Does the time of the first peak have a correlation with the void percentage?
Fig 9. Histogram of all first tau peak times, scaled by how prominent the peak is.
Fig 10. Linear correlation of the time of the tau peak to the void percentage

## Slide 11
Results: Zth(t) for t = 1.5 ms
Model fit ()
Linear fit
Fig 11. Zth vs Voids at 1.58 ms with model fit
Fig 12. Zth vs Voids at 1.58 ms with linear fit

## Slide 12
Results: Zth(t) Correlation at Non-Peak Times
What does Zth look like near steady-state?
Much weaker correlation due to variable thermal resistance of layers between the solder and heat sink
At what time does the void percentage have the highest correlation with Zth?
Peaks at ~3 ms, close to the predicted time constant associated with the chip-to-solder interface!

## Slide 13
Results: Is the Thermal System Truly Linear?
Fig 14. System linearity check by measuring Zth at several values of applied power, as well as at various times.

## Slide 14
Results: Power Cycling
Fig 15. Power cycling results, showing a negative correlation with void percentage.
Chart: Voids Influence on Lifetime
| 0.18382000000000001 | 0.21417999999999998 | 0.17030999999999999 | 0.22097999999999998 | 0.16009000000000001 | 5.2720000000000003E-2 | 0.1016 | 0.13869999999999999 | 8.8999999999999996E-2 | 0.111
Void Content | 19398 | 24693 | 21798 | 23220 | 25977 | 38517 | 34380 | 34539 | 36480 | 37971
Cycling Conditions:
Heating current: 24A
Failure mode: OR
Cause of failure: solder layer fatigue
Initial : 109-116 °C
On-time: 1 sec
Off-time: 1 sec

## Slide 15
Important Results and Discussion
Voids have a distinct effect on thermal resistance, but the absolute change in Rth of the whole package is relatively small.
While our model is able to capture the data trends, it is unclear whether it is truly a good indicator of thermal resistance.
The methodology used for postprocessing appears to be able to accurately measure the thermal resistance of the solder with minimal influence from other layers.
Voids cause a significant decrease in the lifetime of the solder layer during power cycling.

## Slide 16
Future Work
Processing / Computational
Experimental
Finite Element Simulation as a third point of verification for the time constant associated with the chip-to-solder interface
Accurate implementation of structure function method and comparison to the method presented here
Generalization of postprocessing to include arbitrary / pulsed heating current waveforms
Create a general tool / metric to analyze the effect of void size and position
More samples! See if the model is truly accurate, and also examine results for different solder alloys, surface metallizations, and chip types.
Test increased PCB thickness to determine if this causes the first tau peak to increase in prominence

## Slide 17
Acknowledgements
References
Dr. Nicholas Baker
[1] Cosiansi, Fernando. (2016). ISPET: Interface Sintering Process Enhanced Technology. 10.6092/polito/porto/2643767.
[2] Zhou, Zhongfu & Holland, Paul & Igic, Petar. (2008). Compact thermal model of a three-phase IGBT inverter power module. 167-170. 10.1109/ICMEL.2008.4559249.
[3] Bjørn Jørgensen, Asger & Christensen, Nicklas & Dalal, Dipen & Sønderskov, Simon & Bęczkowski, Szymon & Uhrenfeldt, Christian & Munk-Nielsen, Stig. (2017). Reduction of parasitic capacitance in 10 kV SiC MOSFET power modules using 3D FEM. 10.23919/EPE17ECCEEurope.2017.8098962.
[4] Vladimir Székely, Tran Van Bien, Fine structure of heat flow path in semiconductor devices: A measurement and identification method, Solid-State Electronics, Volume 31, Issue 9,1988, Pages 1363-1368, ISSN 0038-1101, https://doi.org/10.1016/0038-1101(88)90099-8. (https://www.sciencedirect.com/science/article/pii/0038110188900998)
Questions?