## Slide 1
Impact of Solder Voids on Power Device Thermal Impedance Using Transient System Analysis
Nathan Carlson
Dept. of Electrical and Computer Engineering
The University of Alabama
ncarlson@crimson.ua.edu
Dr. Nicholas Baker
Dept. of Electrical and Computer Engineering
The University of Alabama
nbaker2@crimson.ua.edu

## Slide 2
What is Die-Attach?
Example power module stack [1]
Die-attach: secures the semiconductor device to the external structure and also conducts main current
Must withstand high temperatures and mechanical stress while also conducting heat and electric current
This is a common point of fatigue failure in power devices
Die-attach can be solder, sinter, or other materials, but we will focus on solder.

## Slide 3
What are Solder Voids?
X-ray image of solder voids underneath a power diode.
Solder voids are small pockets that form in the solder during reflow.
Primarily caused by outgassing of organic compounds in the solder flux, but poor wetting also contributes.
Commonly measured as a “void percentage”, which is the ratio of voided solder area to total area
Can be reduced using vacuum solder machines or other methods

## Slide 4
Main Problem: Vacuum Soldering = $$$
Applications where vacuum soldering may be unattractive:
What impact do voids have?
How does this affect the decision to use vacuum soldering?
Mass production of discrete transistors
Research labs and prototyping

## Slide 5
What We Measured
-------------------- Versus --------------------
Solder voids
Thermal Impedance
Reliability
Fatigue Damage

## Slide 6
Sample Creation
25 Samples
Diode Information:
Two different SAC 305 solder paste (Indalloy 256 and Chipquik SMD291SNL10T4)
‘X’ shaped stencil with 100um thickness
Reflow in convection oven: Manncorp MC 301
Three reflow profiles used (see appendix)
PCB surface metallization: bare Cu
Model: VS-4FD198H06A6BC
Size: 5.03mm X 3.35mm
Rated current: 50A

## Slide 7
Void Percentage Calculation
Selection of voided areas using Fill Tool method.
Void selection with Threshold method.
Traditional threshold method susceptible to chip tilt errors
Fill Tool Method
Capture Xray image of solder
Import into Photoshop
Use the fill tool to select voided areas*
Calculate the number of red pixels vs total pixels
*Fill Tool Threshold settings: 35, 27, 20, 13, 5. Use high settings for large voids and voids with highly contrasted edges.

## Slide 8
Part 1:
Thermal Impedance

## Slide 9
Finite-Element Simulation of Diode
Used IV curve of diode at various temperatures to calculate a lookup table for effective junction conductivity vs local temperature and local current density
Used a “weak contribution” which allows Comsol to solve self-recurrent PDEs.
Diode Electro-Thermal Model
Mesh Refinement
Started with 2 meshes: high-res and low-res. Continually refined low-res mesh until it produced results within 1% of the high-res version.
Diode junction vertical current density (steady-state, mesh A13, 40% void)
Entire model Temperature (degC, steady-state, mesh A13, 40% void)

## Slide 10
Thermal Test Setup
+ -
Example Cooling Curve
Tested currents: 5, 10, 15, 20, 22, 24A
correlated with using second-order polynomial

## Slide 11
Postprocessing: Extraction of Heating Curve
Goal: Given a cooling curve, calculate the heating curve
Assumption 1
Assumption 2
Thermal system is linear and time-invariant (LTI)
System reaches steady-state within 120 seconds
Thermal System
Thermal System
Cooling
Heating

## Slide 12
Why We Can’t Measure Rth Directly
Heating Power
Heat flux through the coldplate is low at the start of the test. We can use Thermal Impedance Zth(t) to measure with lower impact from
Good News!

## Slide 13
Postprocessing: Tau Intensity Calculation
Example diagram of heat flow through a power device
Single Element
Lumped Element
Continuous
Increasing Accuracy
Step response
Equivalent circuit
Step response
Equivalent circuit
Step response
Equivalent circuit
Using , solve for the continuous Tau Intensity function using the method shown in [2].

## Slide 14
Postprocessing: Tau Peak Identification
Purpose of Tau Intensity
The first tau peak (2.24 ms) corresponds to the first material junction from the chip to the solder layer
The time constant peak gives an indication on when the Zth curve should be sampled.
Sample too early () and the heat flux through the solder layer will be too weak. Sample too late () and there will be increased variance due to the heat flux through the coldplate interface.

## Slide 15
Results: First Tau Peak Distribution

## Slide 16
Results: Zth(t)

## Slide 17
Results: Zth(t) for t = 7 ms
Experimental, Linear fit
Simulated

## Slide 18
Results: Zth(t) Correlation at Non-Peak Times
What does Zth look like near steady-state?
At what time does the void percentage have the highest correlation with Zth?
Strongest correlation in the range of 1 – 5 multiples of the time constant
Experimental
Simulated

## Slide 19
Results: Impact Score
Step 1: Using the line of best fit, recognize that Zth can be approximately described by the equation:
Where is the y-intercept, is the slope, and is the void percentage
Step 2: Observe that the total increase due to voids is contained in the term
Step 3: Calculate what percentage of the total thermal impedance is made up of the contribution due to voids and name it the “Impact Score”:

## Slide 20
Results: Is the Thermal System Truly Linear?

## Slide 21
Finite-Element Temperature Variation
Chart: Simulated Steady-State Temperature Variation of Junction (degC)
| 0 | 1 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40
x | 55.98 | 56.096 | 56.855 | 57.933 | 59.14 | 60.428 | 61.851 | 63.838 | 66.294 | 69.439
Temperature variation:
Large temperature gradients introduce mechanical stress on the bondwires, die, and solder
Temperature variation influenced by both size and position of voids, with thermal variance ranging from 56.6 °C to 75.4 °C depending only on position (tested at 10% voids, 24A, steady-state)

## Slide 22
Part 2:
Reliability Testing

## Slide 23
Power Cycling Test Description
Cycling Conditions:
Heating current: 24A
Failure mode:
Initial : 109-116 °C
On-time: 1 sec
Off-time: 1 sec
Main Idea
Observe how solder voids affect the module’s ability to resist thermomechanical fatigue
Purpose
Power modules often experience large temperature swings during operation

## Slide 24
Solder Layer Degradation vs Bondwire Liftoff
Forward Voltage During Power Cycling
We need the solder layer to fail first in order for the test to be accurate
How do we know this is the case?
Another common cause of failure is Bond wire liftoff, where the surface wire connections fall off
If this were to be the cause of failure, there would be sudden jumps in the on-state voltage due to an instantaneous change in electric resistance [3]
This is not the case

## Slide 25
Power Cycling Results
Chart: Voids Influence on Lifetime
| 0.18382000000000001 | 0.21417999999999998 | 0.17030999999999999 | 0.22097999999999998 | 0.16009000000000001 | 5.2720000000000003E-2 | 0.1016 | 0.13869999999999999 | 8.8999999999999996E-2 | 0.111
Void Content | 19398 | 24693 | 21798 | 23220 | 25977 | 38517 | 34380 | 34539 | 36480 | 37971

## Slide 26
Part 3:
Fatigue Damage

## Slide 27
Electron Microscope Setup
Microscope Setup
Device used: Thermo Scientific Axia ChemiSEM
Accelerating voltage: 20 kV
Main detectors used: Concentric Backscatter Detector (CBS)
Test Setup
Compare a new package to one that had been subjected to thermal cycling. Take a cross-section of each chip and image the solder layer using SEM.
What We are Looking For
Cracks in the solder layer and where they form
What the voids look like before vs after cycling
Potential delamination in the PCB
Void shape and size in the non-cycled version

## Slide 28
Healthy Sample

## Slide 29
Healthy Sample

## Slide 30
Cycled Sample

## Slide 31
Cycled Sample

## Slide 32
Cycled Sample

## Slide 33
X-ray Images
Before
After

## Slide 34
Finite-Element Stress Simulation
Solder Layer Von Mieses Stress (20% void, 24A, steady-state)
Solder Layer Von Mieses Stress (0% void, 24A, steady-state)
Chart: Simulted Average Solder Stress vs Void %
| 0 | 1 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40
x | 74624000 | 74409000 | 73945000 | 73542000 | 73223000 | 72894000 | 72668000 | 72548000 | 72505000 | 72565000
Stress model did not include aging effects, a more accurate model for solder is Anand’s Visco-plastic model

## Slide 35
Part 4:
Discussion and Conclusions

## Slide 36
Review of Time Constant Technique
Good
Bad
Provides a consistent sampling time through the peak locations
Time constant matches well with times in which the thermal impedance is most related to solder layer
Implicitly uses a 1-D assumption of heat flow
Uses the foster network interpretation
Future Idea
Use 3-D differential equations to develop a timing method which accounts for heat spreading (not Foster or Cauer)

## Slide 37
Void Impact on Zth
?
While voids definitely have an effect on thermal impedance, the total numerical change is relatively minor

## Slide 38
Power Cycling Overview
Chart: Voids Influence on Lifetime
| 0.18382000000000001 | 0.21417999999999998 | 0.17030999999999999 | 0.22097999999999998 | 0.16009000000000001 | 5.2720000000000003E-2 | 0.1016 | 0.13869999999999999 | 8.8999999999999996E-2 | 0.111
Void Content | 19398 | 24693 | 21798 | 23220 | 25977 | 38517 | 34380 | 34539 | 36480 | 37971
Voids had a much greater impact on power cycling, where an increase of 15% of voids cut the lifetime in half

## Slide 39
Damage Analysis
Voids Appear to facilitate crack formation

## Slide 40
Conclusion
The main drawback of voids is that they reduce the fatigue resistance of the device. The thermal impact of voids is relatively minor.
Exceptions to this rule:
Applications which demand the module to withstand extremely fast transitions in power dissipation
Applications where the thermal resistance is already designed to be ultra-low, so the effect of solder voids is more pronounced

## Slide 41
Future Work
Processing / Computational
Experimental
Include Anand’s Visco-plastic Model
Change the package geometry and materials. See if the time constant peak can still be picked out as easily, and if the new package has a different impact score.

## Slide 42
Acknowledgements
References
Dr. Nicholas Baker
Dr. Andy Mackie and Christine LaBarbera for help with SEM!
Questions?
[1] J. Yang, "Study on solder void for PiP large solder area ultrathin die in solder reflow," 2019 20th International Conference on Electronic Packaging Technology(ICEPT), Hong Kong, China, 2019, pp. 1-4, doi: 10.1109/ICEPT47577.2019.245265.
[2] V. Székely and T. Van Bien, “FINE STRUCTURE OF HEAT FLOW PATH IN SEMICONDUCTOR DEVICES: A MEASUREMENT AND IDENTIFICATION METHOD,” Solid State Electron, vol. 31, no. 9, pp. 1363–1368, 1988.
[3] J. Lehmann, M. Netzel, R. Herzer and S. Pawel, "Method for electrical detection of bond wire lift-off for power semiconductors," ISPSD '03. 2003 IEEE 15th International Symposium on Power Semiconductor Devices and ICs, 2003. Proceedings., Cambridge, UK, 2003, pp. 333-336, doi: 10.1109/ISPSD.2003.1225295.