## Slide 1
Impact of Solder Voids on Power Device Thermal Impedance Using Transient System Analysis
Nathan Carlson
Dept. of Electrical and Computer Engineering
The University of Alabama
ncarlson@crimson.ua.edu
Dr. Nicholas Baker
Dept. of Electrical and Computer Engineering
The University of Alabama
nbaker2@crimson.ua.edu

## Slide 2
Main Problem: Vacuum Soldering = $$$
Applications where vacuum soldering may be unattractive:
What impact do voids have?
How does this affect the decision to use vacuum soldering?
Mass production of discrete transistors
Research labs and prototyping

## Slide 3
What We Measured
-------------------- Versus --------------------
Solder voids
Thermal Impedance
Reliability
Fatigue Damage

## Slide 4
Sample Creation
25 Samples
Diode Information:
Two different SAC 305 solder paste (Indalloy 256 and Chipquik SMD291SNL10T4)
‘X’ shaped stencil with 100um thickness
Reflow in convection oven: Manncorp MC 301
Three reflow profiles used (see appendix)
PCB surface metallization: bare Cu
Model: VS-4FD198H06A6BC
Size: 5.03mm X 3.35mm
Rated current: 50A

## Slide 5
Additional “Side Study”
Jianwei Yang introduced a method in [1] that significantly reduced voids without vacuum.
We tried it on 5 of our samples, and it cut voiding in half (10.7% void average compared to 20.2% average of control group)

## Slide 6
Void Percentage Calculation
Selection of voided areas using Fill Tool method.
Void selection with Threshold method.
Traditional threshold method susceptible to chip tilt errors
Fill Tool Method
Capture Xray image of solder
Import into Photoshop
Use the fill tool to select voided areas*
Calculate the number of red pixels vs total pixels
*Fill Tool Threshold settings: 35, 27, 20, 13, 5. Use high settings for large voids and voids with highly contrasted edges.

## Slide 7
Part 1:
Thermal Impedance

## Slide 8
Thermal Test Setup
+ -
Example Cooling Curve
Tested currents: 5, 10, 15, 20, 22, 24A
correlated with using second-order polynomial

## Slide 9
Postprocessing: Extraction of Heating Curve
Goal: Given a cooling curve, calculate the heating curve
Assumption 1
Assumption 2
Thermal system is linear and time-invariant (LTI)
System reaches steady-state within 120 seconds
Thermal System
Thermal System
Cooling
Heating

## Slide 10
Why We Can’t Measure Rth Directly
Heating Power
Heat flux through the coldplate is low at the start of the test. We can use Thermal Impedance Zth(t) to measure with lower impact from
Good News!

## Slide 11
Postprocessing: Tau Intensity Calculation
Example diagram of heat flow through a power device
Single Element
Lumped Element
Continuous
Increasing Accuracy
Step response
Equivalent circuit
Step response
Equivalent circuit
Step response
Equivalent circuit
Using , solve for the continuous Tau Intensity function using the method shown in [2].

## Slide 12
Postprocessing: Tau Peak Identification
Purpose of Tau Intensity
The first tau peak (2.24 ms) corresponds to the first material junction from the chip to the solder layer
The time constant peak gives an indication on when the Zth curve should be sampled.
Sample too early () and the heat flux through the solder layer will be too weak. Sample too late () and there will be increased variance due to the heat flux through the coldplate interface.

## Slide 13
Results: First Tau Peak Distribution

## Slide 14
Results: Zth(t) for t = 7 ms
Linear fit

## Slide 15
Results: Zth(t) Correlation at Non-Peak Times
What does Zth look like near steady-state?
Almost no correlation due to variable thermal resistance of caused by the cold plate connection
At what time does the void percentage have the highest correlation with Zth?
Strongest correlation in the range of 1 – 5 multiples of the time constant

## Slide 16
Results: Impact Score
Step 1: Using the line of best fit, recognize that Zth can be approximately described by the equation:
Where is the y-intercept, is the slope, and is the void percentage
Step 2: Observe that the total increase due to voids is contained in the term
Step 3: Calculate what percentage of the total thermal impedance is made up of the contribution due to voids and name it the “Impact Score”:

## Slide 17
Results: Is the Thermal System Truly Linear?

## Slide 18
Part 2:
Reliability Testing

## Slide 19
Power Cycling Test Description
Cycling Conditions:
Heating current: 24A
Failure mode:
Initial : 109-116 °C
On-time: 1 sec
Off-time: 1 sec
Main Idea
Observe how solder voids affect the module’s ability to resist thermomechanical fatigue
Purpose
Power modules often experience large temperature swings during operation

## Slide 20
Solder Layer Degradation vs Bondwire Liftoff
Forward Voltage During Power Cycling
We need the solder layer to fail first in order for the test to be accurate
How do we know this is the case?
Another common cause of failure is Bond wire liftoff, where the surface wire connections fall off
If this were to be the cause of failure, there would be sudden jumps in the on-state voltage due to an instantaneous change in electric resistance [3]
This is not the case

## Slide 21
Power Cycling Results
Chart: Voids Influence on Lifetime
| 0.18382000000000001 | 0.21417999999999998 | 0.17030999999999999 | 0.22097999999999998 | 0.16009000000000001 | 5.2720000000000003E-2 | 0.1016 | 0.13869999999999999 | 8.8999999999999996E-2 | 0.111
Void Content | 19398 | 24693 | 21798 | 23220 | 25977 | 38517 | 34380 | 34539 | 36480 | 37971

## Slide 22
Part 3:
Fatigue Damage

## Slide 23
Electron Microscope Setup
Microscope Setup
Device used: Thermo Scientific Axia ChemiSEM
Accelerating voltage: 20 kV
Main detectors used: Concentric Backscatter Detector (CBS)
Test Setup
Compare a new package to one that had been subjected to thermal cycling. Take a cross-section of each chip and image the solder layer using SEM.
What We are Looking For
Cracks in the solder layer and where they form
What the voids look like before vs after cycling
Potential delamination in the PCB
Void shape and size in the non-cycled version

## Slide 24
Healthy Sample

## Slide 25
Healthy Sample

## Slide 26
Cycled Sample

## Slide 27
Cycled Sample

## Slide 28
Cycled Sample

## Slide 29
X-ray Images
Before
After

## Slide 30
Part 4:
Discussion and Conclusions

## Slide 31
Review of Time Constant Technique
Good
Bad
Provides a consistent sampling time through the peak locations
Time constant matches well with times in which the thermal impedance is most related to solder layer
Implicitly uses a 1-D assumption of heat flow
Uses the foster network interpretation
Future Idea
Use 3-D differential equations to develop a timing method which accounts for heat spreading (not Foster or Cauer)

## Slide 32
Void Impact on Zth
?
While voids definitely have an effect on thermal impedance, the total numerical change is relatively minor

## Slide 33
Power Cycling Overview
Chart: Voids Influence on Lifetime
| 0.18382000000000001 | 0.21417999999999998 | 0.17030999999999999 | 0.22097999999999998 | 0.16009000000000001 | 5.2720000000000003E-2 | 0.1016 | 0.13869999999999999 | 8.8999999999999996E-2 | 0.111
Void Content | 19398 | 24693 | 21798 | 23220 | 25977 | 38517 | 34380 | 34539 | 36480 | 37971
Voids had a much greater impact on power cycling, where an increase of 15% of voids cut the lifetime in half

## Slide 34
Damage Analysis
Voids Appear to facilitate crack formation

## Slide 35
Conclusion
The main drawback of voids is that they reduce the fatigue resistance of the device. The thermal impact of voids is relatively minor.
Exceptions to this rule:
Applications which demand the module to withstand extremely fast transitions in power dissipation
Applications where the thermal resistance is already designed to be ultra-low, so the effect of solder voids is more pronounced

## Slide 36
Future Work
Processing / Computational
Experimental
Finite element simulation
New postprocessing method which accounts for heat spreading
Change the package geometry and materials. See if the time constant peak can still be picked out as easily, and if the new package has a different impact score.

## Slide 37
Acknowledgements
References
Dr. Nicholas Baker
Dr. Andy Mackie and Christine LaBarbera for help with SEM!
Questions?
[1] J. Yang, "Study on solder void for PiP large solder area ultrathin die in solder reflow," 2019 20th International Conference on Electronic Packaging Technology(ICEPT), Hong Kong, China, 2019, pp. 1-4, doi: 10.1109/ICEPT47577.2019.245265.
[2] V. Székely and T. Van Bien, “FINE STRUCTURE OF HEAT FLOW PATH IN SEMICONDUCTOR DEVICES: A MEASUREMENT AND IDENTIFICATION METHOD,” Solid State Electron, vol. 31, no. 9, pp. 1363–1368, 1988.
[3] J. Lehmann, M. Netzel, R. Herzer and S. Pawel, "Method for electrical detection of bond wire lift-off for power semiconductors," ISPSD '03. 2003 IEEE 15th International Symposium on Power Semiconductor Devices and ICs, 2003. Proceedings., Cambridge, UK, 2003, pp. 333-336, doi: 10.1109/ISPSD.2003.1225295.